## Slide 1: Fire design
NOB021
doc. Ing. Martin Vild, Ph.D.
4/2026

## Slide 2: Prezentuje
doc. Ing. Martin Vild, Ph.D.
IDEA StatiCa – Product Owner
VUT FAST – Docent
Výzkum:
Přípoje ocelových konstrukcí
Metoda konečných prvků
Scopus Author ID: 56188615700
Člen komisí:
CEN/TC 250/SC 3/WG 8 "Evolution of EN 1993-1-8 - Joints and connections“
ECCS TC10 “Structural Connections”
Web:
https://www.fce.vutbr.cz/KDK/vild.m/
email: martin.vild@vutbr.cz
Kancelář: C203

## Slide 3: Contents
Introduction:
  Design codes
  Accidental situation
  Concepts
Fire curves
Material properties
Fire protection
Steel temperature

## Slide 4: Design codes
EN 1991-1-2 (thermal actions)
EN 1993-1-2 – Eurocode 3: Design of steel structures - Part 1-2: General rules - Structural fire design
EN 1992-1-2 (concrete), EN 1994-1-2 (composite), EN 1995-1-2 (timber)
Building regulations (compartments, escape routes, fire walls)
Standard prescriptive
Simple
For standard design cases
Neglects:
System response
Connections
Thermal stresses (elongation/shrinkage)
Performance-based
Where standard prescriptive does not make sense (train/bus station…)
Attempt to model:
Real fire hazards
Actual building response
Specified performance
Time-consuming design
Economic, safe

## Slide 5: Accidental load
Safety factor
Often explosion + fire or crash + fire
Static loads – simplified:

## Slide 6: Weakening concepts
Steel – whole plate or member
Timber – charring around
Heavy/light
Concrete – from around, high mass, reinforcement

## Slide 8: Concept
Passive/active fire protection
Compartmentalization
People must escape first
Firefighters are safe while fighting the fire
Building collapses inside
Surrounding buildings do not catch fire

## Slide 9: Concept
There are many ways how to deal with fire safety:
People escape very fast (e.g., UK)
Building lasts long during fire (e.g., CZ)
  Fire protection (impact on environment and schedule)
  A lot of mass (larger beams than needed for SLS+ULS)

## Slide 10: Fire stages
Ignition (Sprinklers)
Growth
Flashover
Fully-developed fire
Decay
ISO

## Slide 11: Fire curves
Standard fire curve ISO 834 (EN 1991-1-2)
AISC fire curve ASTM E119:

## Slide 12: Fire curves
External fire curve (EN 1991-1-2)
Hydrocarbon curve (EN 1991-1-2)

## Slide 13: Material properties – Steel
Chart: 
| 20 | 100 | 150 | 200 | 300 | 400 | 500 | 600 | 700 | 800 | 900 | 1000
Bolts | 1 | 0.968 | 0.952 | 0.935 | 0.903 | 0.775 | 0.55 | 0.22 | 0.1 | 0.067 | 0.033 | 0
Welds | 1 | 1 | 1 | 1 | 1 | 0.876 | 0.627 | 0.378 | 0.13 | 0.074 | 0.018 | 0
fy | 1 | 1 | 1 | 1 | 1 | 0.78 | 0.47 | 0.23 | 0.11 | 0.06 | 0.04 | 0.02 | 0

## Slide 14: Material properties – Steel
Phase transformation
Melts at about 1450 ˚C

## Slide 15: Fire protection
https://fgg-web.fgg.uni-lj.si/~/pmoze/esdep/master/wg04b/l0400.htm

## Slide 16: Temperature
Unprotected internal steelwork
Internal steelwork insulated by fire protection material

## Slide 17: Temperature

## Slide 18: Design workflow
Time classes – 15, 30, 45, 60…240 min (EN 13501-2)
Fire curves
Loading (accidental)
Temperature of air → temperature of steel
Reduce material properties
Calculate resistances
Increase sizes / add fire protection / add restraints

## Slide 19: Beam – verification
Chart: Temperature [°C]
| 20 | 400 | 500 | 600
AM | 72.28 | 44.6 | 37.56 | 19.96
Shell | 64.54 | 40.1 | 33.18 | 17.34
CBFEM | 66.55 | 45 | 37.51 | 20.62
Buckling! E dropping fast

## Slide 20: Column – verification
Length L (m) | HEB 300 - PP - 600°C |  | Boundary conditions | HEB 300 - 6 m - 500°C | 
 | AM | CBFEM |  | AM | CBFEM
4 | 1129 | 1020 | PP | 1347 | 1238
6 | 737 | 660 | FP | 1915 | 1742
7 | 596 | 550 | FF | 2334 | 2226

## Slide 21: Member design
https://www.scia.net/en/scia-engineer/fact-sheets/steel-design/sensd05-steel-fire-resistance-design

## Slide 22: Task 1
Calculate the buckling resistance of simply supported column HEA 200 with the length of 3 m at 15 min of standard fire curve in:
SCIA Engineer or Dlubal using code calculations
IDEA StatiCa Member using GMNIA

## Slide 23: Connections
Temperature of steel plates = temperature of bolts or welds
Safe assumption (there is more material, slower heating)
Loading:
Heating = expansion
Cooling = shrinkage – may be governing – large tensile forces in the members, which elongate and then shrink

## Slide 24: Connections – validation
Specimen | θ (°C) | Experiment |  |  | Eurocode | 
 |  | Failure Loads [kN] | Mean Resistance [kN] | Failure Mode | Resistance [kN] | Failure Mode
Test 1 | 20 | 297.8 | 297.8 | Bolts in shear | 241.2 | Bolts in shear
Test 2 |  | 146.7 | 148.4 | Bolts in shear | 120.6 | Bolts in shear
Test 3 |  | 150.1 |  |  |  | 
Test 4 | 400 | 106.4 | 110.8 | Bolts in shear | 93.6 | Bolts in shear
Test 5 |  | 122.6 |  |  |  | 
Test 6 |  | 103.4 |  |  |  | 
Test 7 | 600 | 36.7 | 32.7 | Bolts in shear | 26.9 | Bolts in shear
Test 8 |  | 33.9 |  |  |  | 
Test 9 |  | 27.5 |  |  |  | 
Chart: Temperature [°C]
| 20 | 400 | 600
Experiment | 148.6 | 110.8 | 32.7
CBFEM | 111.75 | 106.4 | 29.7

## Slide 25: Connections – validation
a) T-10-600; b) T-15-500; c) T-20-500
Chart: Flange thickness [mm]
| 10 | 15 | 20 | 10 | 15 | 20 | 10 | 15 | 20
Experiment | 158.5 | 291 | 460.7 | 137 | 177 | 335 | 43.9 | 77.8 | 187
CBFEM | 117.1 | 204.4 | 391 | 85.2 | 150 | 278 | 46.6 | 63.3 | 117

## Slide 26: IDEA StatiCa Connection

## Slide 27: IDEA StatiCa Connection
Bolts and welds have the temperature of the hotter connected plate

## Slide 28: IDEA StatiCa Connection
Perhaps too safe (accidental design situation)

## Slide 29: Task 2
Design an end plate beam-to-column connection to resist 60% of beam bending resistance (ULS).
Design a fire protection, so that the connection resists 70% of the original load for time class R90.
Design members and connection, so that no fire protection is needed for R30 for the same load.

## Slide 30: Further reading
https://fgg-web.fgg.uni-lj.si/~/pmoze/esdep/master/wg04b/toc.htm
https://people.fsv.cvut.cz/~wald/fire/ifer/benchmark/index.htm
https://eurocodes.jrc.ec.europa.eu/sites/default/files/2022-06/03a-VASSART-EC-FireDesign-WS.pdf